RESEARCH COMPLETION CERTIFICATE

Certified that the research work contained in this thesis titled, Kinetic Study of Transesterification of Castor Oil Using Mn Doped ZnO Nano-Particles has been carried out and completed by Muhammad Zahid Mukhtar, ID: S2017140007.The quantum and the quality of the work contained in this thesis are adequate for the award of Degree of MS.

# _____________________			___________________

# Supervisor						External Examiner

# Dr Sammia Shahid

Associate Professor

Dean (Research)

___________________________   		   	 ___________________________

## Chairperson                                           	Dean

## Dr. Ayesha Mohy-Ud-Din	             	Dr Muhammad Azhar Iqbal

## Associate Professor                                	 Professor

Department of Chemistry,   		    	School of Science,

UMT, Lahore.				    	UMT, Lahore.

## DECLARATION

## I, Muhammad Zahid Mukhtar S/O Mukhtar Ahmad ID: S2017140007                     Session 2017-2019 hereby declare that the matter printed in the thesis titled “Kinetic Study of Transesterification of Castor Oil Using Mn Doped ZnO Nano-Particles” is my own work and has not been printed, published and submitted as research work, thesis or publication in any form in any University, Research institution etc. in Pakistan or Abroad.

## Dated: ______________                                 ________________________

## (Muhammad Zahid Mukhtar)

I dedicate this research thesis to my

Abbu G

Mukhtar Ahmad (Late), May Allah bless him high rank in Jannat-ulFirdous

ACKNOWLEDGMENT

In the name of Allah (SWT), the most beneficent and the merciful, none is worthy of worship except He, the ever living, the one who sustains and protects all exists. He is the source of every kind of Knowledge. All praises and thanks be to Allah, the Lord of mankind in all worlds.

A great respect for Muhammad (S.A.W), the last messenger of Allah on earth, he is forever guidance for the mankind, the example of ideal human being, and a great teacher who guided humans towards the light of knowledge.

I am honored to pay thanks to Dr. Muhammad Azhar Iqbal (Dean School of Sciences) on his significance guidance. I am thankful from the core of my heart to the Dr Sammia Shahid, Dean of Research, University of Management and Technology (UMT), Lahore. She is the role model, source of motivation and the symbol  of love, affection, guidance and hope for me during this research work. I am also thankful to Prof. Dr Ayesha Mohyuddin Chairperson of Chemistry Department, (UMT), Lahore on her sincere support and guidance. I am thankful to all faculty and  support staff working in chemistry department of UMT Lahore.

I extended my gratitude to my Father Mukhtar Ahmad (Late) and my Father in Law Hafeez-ur-Rehman  (Late) who left us during this research work in 2019. They were very keen and prayed for our achievements. May Allah bless them High rank in Jannah

I am really thankful to my friends’ family and especially my classmate and my wife Ms. Afifa on her unconditional support may Allah bless her best reward in this and the next world.

ABSTRACT

A paradigm shift from ongoing industrial development to environmental friendly resources  have been observed in scientific researchers from last two decades due to rapid increase in average temperature of the earth called global warming.  A threat of extinction of natural fuel resources is another scaring issue in the line of human development. The alarming situation of the environmental changes increased the apprehension of the scientist to phase out traditional energy recourses and move on environmental friendly biofuels. In this study, a non-edible castor oil was transeterified by methanol in the presence of Mn doped ZnO nanocatalyst. Heterogeneous Nanocatalyst was prepared by sono-chemical method. XRD was consulted to get information abouit the crystal lattices, EDX was performed to find out purity of nanocatalyst produced while TEM was used to investigate morphology of the crystals and the average size of the nanoparticles produced. Transesterification reaction was studied in different conditions of temperature, methyl alcohol to castor oil ratio, amount of catalyst to get optimim conditions at maximum yield of biodiesel produced. Maximum yield (90.3%) of biodiesel was observed at 55, oil to methanol ratio 1: 12 while the amount of nanocatalyst taken was 1.2gm by weight.1st order kinetic model was found most suitable, keeping in view the applied reaction conditions. The kinetic model was extended to calculate rate constant, activation energy, enthalpy of the reaction, entropy and Gibb’s free energy. The thermodynamical factors revealed that transesterification reaction was endothermic and need constant heat energy while converting the reactants into product.

CONTENTS

Acknowledgements……………………………………………...v

Abstract…………………………………………………………...vi

Table of contents……………………………………………….vii

List of figures…………………………………………………....ix

List of tables……………………………………………………...x

List of Abbriviations ……………………………………….…....xi

Chapter-1		Introduction

  - Background and Motivation……………………………………………...1

  - Objectives of Study……………………………………………………....2

  - Outline of the work………………………………………………………2

  - Resources of Energy……………………………………………………...2

  - Biodiesel………………………………………………………………….3

  - Some important features of Biodiesel…………………………………..4

  - Challenges………………………………………………………………..5

  - Large Scale Production of Biodiesel…………….………………………6

  - Edible and non edible oils………………………………………………..6

  - Global Consumption of biodiesel ………………………………………...6

  - Properties of Biodiesel……………………………………………...….....7

  - Raw Material of Biodiesel…………………………………………..…....9

  - Common Methods of biodiesel production…………………………..…10

  - Transesterification…………………………………………………….…10

  - Castor Oil……………………………………………………………...….11

  - Catalyst………………………………………………………………...….12

  - Nano catalysts………………………………………………………...….13

  - Metal oxide Nanocatalyst………………………………………….….…14

  - Zinc Oxide Nanocatalyst……………………………………………..….15

  - Preparation of Zinc Oxide Nanoparticels…………………………….…16

  - Mn doped Zinc Oxide nanoparticles……………………………………16

  - Kinetics of Biodiesel…………………………………………………..…16

Chapter-2		Literature Review

2.0	Literature Review……………………………………....………….……18

Chapter-3		Material &Methods

3.1. 	Mode of action………………………………………………………….26

3.2	List of Apparatus………………………....……………………………..26

3.3	List of instruments…………………………………………………..…..27

3.4	List of chemicals……………………………………………..…….……30

3.5	Formation of nanoparticles…………………………………..………….30

3.6	Characterization Techniques………………………………….……….31

3.7	Application of nanoparticles as nanoctalyst…………….…………….32

3.8	Production of Biodiesel from nanocatalyst……………….……….…..32

3.9	Some Important Factors effecting biodiesel production………….…...33

3.10	Calculation of Yield…………………………….…………………...….34

3.11	Physicochemical characteristics of biodiesel……………………..……35

3.12	Kinetics involved in Transesterification………………...……..….36

Chapter-4		Results and Discussion

4.1	Characterization of Mn doped ZnO nanoparticles………………………40

4.2	Physicochemical properties of biodiesel………………...………………43

4.3	Factors Effecting Yield of Biodiesel………………..……………….…..45

4.4	Kinetics of Tranesterification Reaction……………...………………….48

4.5	Conclusion………………………………...…………………………….62

References …………………………………………...…….………63

LIST OF FIGURES

No.	Description							Page

1	Commercial process of biodiesel production					10

2	Catalytic action on activation energy of a chemical reaction			12

3	Applications of Nanocatalyst							15

4	Filtration of MnZnO  nanoparticles prepared in Laboratory			31

5	Determination of FFA in castor oil					39

6	XRD spectra of Mn doped ZnO nanoparticles				40

7	TEM of Mn doped ZnO nanoparticles					42

8	TEM of Mn doped ZnO nanoparticles					43

9	EDX Spectra of Mn doped Zno nanoparticles				46

10	Catalyst amount and biodiesel yield						47

11	Effect of oil-methanol ratio on biodiesel yield				48

12	Effect of temperature on biodiesel yield					52

13	Plot of data time (t) intervals against amount of FFA			55

14	Effect of reaction time in minutes on FFA Concentration 			55

15	Linear portion of concentration and Reaction time in minutes		57

16	and 1/T to get slope (activation energy) of the reaction		59

17	and 1/T to get slope (enthalpy) of the reaction				61

18	Gibb’s energy plot against different reaction temperatures			61

LIST OF TABLES

No.		Description							Page

1	Biodiesel production by different countries during year 2009-10		07

2	Properties of biodiesel with standard values					08

3	List of Apparatus used for experimental work				26

4	List of Instruments experienced in practical work				27

5	List of Chemicals used in preparation of MnZnO nanoparticles		30

6	Chemicals used to prepare Biodiesel						32

7	Chemicals used to FFA calculation in Caster oil				37

8	Physicochemical properties of Biodiesel produced from castor oil.		44

9	Yield of biodiesel against amount of catalyst					45

10	Effect of methanol on %age yield of biodiesel 				46

11	Effect of temperature on %age yield of biodiesel				47

12	Change in concentration of FFA with time intervals taken in minutes	52

13	Calculated values of FFA and rate constant of at 50			53

14	Calculated values of FFA and rate constant of at 55			54

15	Calculated values of FFA and rate constant at 60				54

16	 and (1/T) values used to calculate activation energy by 		56

17         	& 1//T of the reaction by eyring equation				58

18	Gibb’s energy values 	at different temperatures			61

LIST OF ABBREVIATIONS

| Abbreviation | Name |
| --- | --- |
| IEO | International Energy Outlook |
| WEF | World Energy Forum |
| EU | European Union |
| FAME | Fatty Acids Methyl Ester |
| XRD | X-ray Diffraction |
| SEM | Scanning Electron Microscope |
| TEM | Transmission Electron Microscope |
| UV | Ultra Violet |
| EDX | Electron Dispersive X-ray |
| RSM | Response Surface Methodology |
| FTIR | Fourier Transform Infra red Spectroscopy |
| AFM | Atomic Force Microscopy |
| GCMS | Gas Chromatography Mass Spectroscopy |
| SWOT | Strength Weakness Opportunities and Threats |
| UMT | University of Management and Technology |
| MnZnO | Manganese doped Zinc Oxide naoparticels |