CONTENTS

List of Tables										Iv

List of Figures										v

Abbreviations										viii

Acknowledgements									x

Abstract										xi

- INTRODUCTION                                                                      1-13

  - Nanoparticles								1

    - Types of Nanoparticles						1

    - Preparation Methods						2

  - Zinc Oxide Nanoparticles							3

    - Methods of Preparation						3

    - Functions								4

  - Graphitic Carbon Nitride							4

    - Synthesis of g-C3N4							4

    - Applications of g-C3N4						5

  - Nanocomposites								6

    - Classification of Nanocomposites					6

      - Non-Polymer Based Nanocomposites				7

      - Polymer Based Nanocomposites				7

    - Techniques								8

    - Applications							9

  - Photocatalytic Activity							10

  - Characterization Techniques						10

    - Scanning Electron Microscopy (SEM)				11

    - Transmission Electron Microscopy (TEM)				11

    - X-Ray Diffraction (XRD)						11

    - Fourier Transform Infrared Spectroscopy (FTIR)			12

    - UV-Visible Spectroscopy						12

  - Aims and objectives							13

- LITERATURE REVIEW					      14-21

- MATERIALS AND METHODS				      22-28

  - Chemical and Reagents							22

  - Apparatus and Glassware							22

  - Synthesis of Pure ZnO Nanoparticles					23

  - Synthesis of Cr-doped ZnO						24

  - Synthesis of Sulfur doped Graphitic Carbon Nitride 			25

  - Synthesis of Nanocomposite Cr-doped ZnO/Sulfur-doped  g-C3N4	25

  - Photocatalytic Activity of Nanoparticles and Nanocomposites`		26

- RESULTS AND DISCUSSIONS				      29-72

  - X-Ray Diffraction (XRD)							29

    - XRD of ZnO Nanoparticles						29

    - XRD of 5% Cr-doped ZnO Nanoparticles				30

    - XRD of Sulfur-doped g-C3N4					31

  - Scanning Electron Microscope (SEM)					32

    - SEM of ZnO Nanoparticles						32

    - SEM of Sulfur-doped g-C3N4					33

    - SEM of 5% Cr-doped ZnO						34

  - Fourier Transform Infrared Spectroscopy (FTIR)				35

    - FTIR of ZnO Nanoparticles					35

    - FTIR of 5% Cr-doped ZnO Nanoparticles				36

    - FTIR of Sulfur-doped g-C3N4					37

    - FTIR of 15% Cr-doped  ZnO Nanoparticles/Sulfur-doped

g-C3N4								38

  - UV-Visible spectroscopy							39

    - Photocatalytic Activity of ZnO Nanoparticles			39

    - Photocatalytic Activity of 1% Cr-doped ZnO Nanoparticles 	40

    - Photocatalytic Activity of 3% Cr-doped ZnO Nanoparticles	41

    - Photocatalytic Activity of 5% Cr-doped ZnO Nanoparticles	42

    - Photocatalytic Activity of 7% Cr-doped ZnO Nanoparticles	43

    - Photocatalytic Activity of 9% Cr-doped ZnO Nanoparticles	44

    - Comparison of Photocatalytic Activity of Cr-doped

Nanoparticles at 0 minute						45

    - Comparison of Photocatalytic Activity of Cr-doped

Nanoparticles at 30 minute						46

    - Comparison of Photocatalytic Activity of Cr-doped

Nanoparticles after 1 hour						47

    - Comparison of Photocatalytic Activity of Cr-doped

Nanoparticles after 1 hour 30 minutes				48

    - Comparison of Photocatalytic Activity of Cr-doped

Nanoparticles after 2 hours						49

    - Comparison of Photocatalytic Activity of Cr-doped

Nanoparticles after 2 hours 30 minutes 				50

    - Comparison of Photocatalytic Activity of Cr-doped

Nanoparticles after 3 hours						51

    - Comparison of Photocatalytic Activity of Cr-doped

Nanoparticles after 3 hour 30 minutes 		            	52

    - Photocatalytic Activity of S-doped g-C3N4			53

    - Photocatalytic Activity of 5% Cr-doped ZnO Nanocomposite

with S-doped  g-C3N4						54

    - Photocatalytic Activity of 10% Cr-doped ZnO Nanocomposite

with S-doped  g-C3N4						55

    - Photocatalytic Activity of 15% Cr-doped ZnO Nanocomposite

with S-doped  g-C3N4						56

    - Photocatalytic Activity of 20% Cr-doped ZnO Nanocomposite

with S-doped  g-C3N4						57

    - Comparison of Photocatalytic Activity of Cr-doped Nano-

Composite with S-doped g-C3N4 in Dark				58

    - Comparison of Photocatalytic Activity of Cr-doped Nano-

Composite with S-doped g-C3N4 after 30 minutes			59

    - Comparison of Photocatalytic Activity of Cr-doped Nano-

Composite with S-doped g-C3N4 after 1 hour			60

    - Comparison of Photocatalytic Activity of Cr-doped Nano-

Composite with S-doped g-C3N4 after 1 hour 30 minutes 		61

    - Comparison of Photocatalytic Activity of Cr-doped Nano-

Composite with S-doped g-C3N4 after 2 hours			62

    - Comparison of Photocatalytic Activity of Cr-doped Nano-

Composites with S-doped g-C3N4 after 2 hours 30 minutes	63

    - Comparison of Photocatalytic Activity of Cr-doped Nano-

Composites with S-doped g-C3N4 after 3 hours			64

    - Tauc Plot of ZnO							65

    - Tauc Plot of 1% Cr-doped ZnO					66

    - Tauc Plot of 3% Cr-doped ZnO					67

    - Tauc Plot of 5% Cr-doped ZnO					68

    - Tauc Plot of 7% Cr-doped ZnO					69

    - Tauc Plot of 9% Cr-doped ZnO					70

    - Tauc Plot of 15% Cr-doped ZnO/ S-doped g-C3N4 		71

  - Conclusion									72

REFERENCES								      73-77

List of Tables

| Serial No. | Title | Page No. |
| --- | --- | --- |
| 1 | List of Chemicals | 22 |
| 2 | List of Glassware and Instruments | 22-23 |

List of Figures

| Figure No. | Title | Page No. |
| --- | --- | --- |
| 1.1 | Types of nanoparticles | 1 |
| 1.2 | Functions of ZnO | 2 |
| 1.3 | Synthesis techniques of nanoparticles | 2 |
| 1.4 | Preparation methods for g-C3N4 | 5 |
| 1.5 | Photocatalytic functions of g-C3N4 | 5 |
| 1.6 | Types of Nanocomposites | 7 |
| 1.7 | Types of Non-polymer based nanocomposites | 7 |
| 1.8 | Types of polymer based nanocomposites | 8 |
| 1.9 | Synthesis methods of nanocomposites | 9 |
| 3.1 | ZnO nanoparticles | 24 |
| 3.2 | Autoclave for synthesis of nanoparticles | 24 |
| 3.3 | Muffle furnace for calcination | 25 |
| 3.4 | Drying of nanoparticles | 26 |
| 3.5 | UV-Visible spectrophotometer | 27 |
| 3.6 | The Sonicator | 27 |
| 3.7 | Different steps of photocatalytic activity (a) sample placed in dark (b) sample placed in sunlight for Photocatalysis (c) dye degradation in sunlight during photocatalysis | 28 |
| 3.8 | SEM sample storage stub and tube | 28 |
| 4.1 | XRD of ZnO | 29 |
| 4.2 | XRD of 5% Cr-doped ZnO NPs | 30 |
| 4.3 | XRD of Sulfur-doped g-C3N4 | 31 |
| 4.4 | SEM of ZnO nanoparticles | 32 |
| 4.5 | SEM of Sulfur doped g-C3N4 | 33 |
| 4.6 | SEM of 5% Cr-doped ZnO | 34 |
| 4.7 | FTIR of ZnO | 35 |
| 4.8 | FTIR Spectrum of 5% Cr-doped ZnO | 36 |
| 4.9 | FTIR of Sulfur doped g-C3N4 | 37 |
| 4.10 | FTIR of 15% nanocomposite | 38 |
| 4.11 | Photocatalytic activity of ZnO NPs | 39 |
| 4.12 | Photocatalytic activity of 1% Cr-doped ZnO NPs | 40 |
| 4.13 | Photocatalytic activity of 3% Cr-doped ZnO NPs | 41 |
| 4.14 | Photocatalytic activity of 5% Cr-doped ZnO NPs | 42 |
| 4.15 | Photocatalytic activity of 7% Cr-doped ZnO NPs | 43 |
| 4.16 | Photocatalytic activity of 9% Cr-doped ZnO NPs | 44 |
| 4.17 | Comparison of photocatalytic activity of Cr-doped ZnO NPs with ZnO after 0 min | 45 |
| 4.18 | Comparison of photocatalytic activity of Cr-doped ZnO NPs with ZnO after 30 min | 46 |
| 4.19 | Comparison of photocatalytic activity of Cr-doped ZnO NPs with ZnO after 60 min | 47 |
| 4.20 | Comparison of photocatalytic activity of Cr-doped ZnO NPs with ZnO after 90 min | 48 |
| 4.21 | Comparison of photocatalytic activity of Cr-doped ZnO NPs with ZnO after 120 min | 49 |
| 4.22 | Comparison of photocatalytic activity of Cr-doped ZnO NPs with ZnO after 150 min | 50 |
| 4.23 | Comparison of photocatalytic activity of Cr-doped ZnO NPs with ZnO after 180 min | 51 |
| 4.24 | Comparison of photocatalytic activity of Cr-doped ZnO NPs with ZnO after 210 min | 52 |
| 4.25 | Photocatalytic activity of S-doped g-C3N4 NPs | 53 |
| 4.26 | Photocatalytic activity of 5% Cr-doped ZnO nanocomposite with S-doped g-C3N4 | 54 |
| 4.27 | Photocatalytic activity of 10% Cr-doped ZnO nanocomposite with S-doped g-C3N4 | 55 |
| 4.28 | Photocatalytic activity of 15% Cr-doped ZnO nanocomposite with S-doped g-C3N4 | 56 |
| 4.29 | Photocatalytic activity of 20% Cr-doped ZnO nanocomposite with S-doped g-C3N4 | 57 |
| 4.30 | Comparison of photocatalytic activity of Cr-doped ZnO nanocomposite with S-doped g-C3N4 and 5% Cr-doped ZnO after 0 min | 58 |
| 4.31 | Comparison of photocatalytic activity of Cr-doped ZnO nanocomposite with S-doped g-C3N4 and 5% Cr-doped ZnO after 30 min | 59 |
| 4.32 | Comparison of photocatalytic activity of Cr-doped ZnO nanocomposite with S-doped g-C3N4 and 5% Cr-doped ZnO after 60 min | 60 |
| 4.33 | Comparison of photocatalytic activity of Cr-doped ZnO nanocomposite with S-doped g-C3N4 and 5% Cr-doped ZnO after 90 min | 61 |
| 4.34 | Comparison of photocatalytic activity of Cr-doped ZnO nanocomposite with S-doped g-C3N4 and 5% Cr-doped ZnO after 120 min | 62 |
| 4.35 | Comparison of photocatalytic activity of Cr-doped ZnO nanocomposite with S-doped g-C3N4 and 5% Cr-doped ZnO after 150 min | 63 |
| 4.36 | Comparison of photocatalytic activity of Cr-doped ZnO nanocomposite with S-doped g-C3N4 and 5% Cr-doped ZnO after 180 min | 64 |
| 4.37 | Tauc plot of ZnO | 65 |
| 4.38 | Tauc plot of 1% Cr-doped ZnO | 66 |
| 4.39 | Tauc plot of 3% Cr-doped ZnO | 67 |
| 4.40 | Tauc plot of 5% Cr-doped ZnO | 68 |
| 4.41 | Tauc plot of 7% Cr-doped ZnO | 69 |
| 4.42 | Tauc plot of 9% Cr-doped ZnO | 70 |
| 4.43 | Tauc plot of 15% composite | 71 |

LIST OF ABBREVIATION

| CVD | Chemical vapor deposition |
| --- | --- |
| PVD | Physical vapor deposition |
| L-B films | Langmuir-Blodgett films |
| ZnO | Zinc Oxide |
| g-C3N4 | Graphitic Carbon Nitride |
| SEM | Scanning electron microscopy |
| TEM | Transmission electron microscopy |
| XRD | X-ray Diffraction |
| FT-IR | Fourier-Transform infrared spectroscopy |
| UV-Vis | Ultraviolet-visible spectroscopy |
| TG-DTA | Thermogravimetry/Differential Thermal Analysis |
| SLS | Static light scattering |
| EELS | Electron energy loss spectroscopy |
| HRTEM | High-resolution transmission electron microscopy |
| EDS/EDX | Energy Dispersive Spectroscopy/Energy Dispersive X-ray |
| BPA | Bisphenol A |
| SPR | Surface Plasmon resonance |
| AFM | Atomic force microscopy |
| TCN | Tetracyanonickelate Ion |
| PEC | Priority existing chemical |
| UV-VIS-NIR | Ultraviolet–visible–near infrared spectroscopy |
| VSM | Vibrating sample magnetometer |
| XPS | X-ray photoelectron spectroscopy |
| Rh B | Rhodamine B |
| PL | Photoluminescence |
| MO | Molecular orbital |
| POPs | Persistent organic pollutants |
| MB | Methylene blue |

ACKNOWLEDGEMENTS

Firstly, I am thankful to Allah Almighty for giving me strength and courage at each and every step in accomplishment of this thesis. Countless salutations are upon the Holy Prophet (Peace be upon him) who enabled me to recognize my Creator and declared it to be an obligatory duty of every Muslim to acquire knowledge.

I would like to honor special regards to Professor Dr. Muhammad Azhar Iqbal Dean of school of Science UMT, who takes special interest in research activities.

I am thankful to my inspiration Dr. Ayesha Mohyuddin, Chairperson of Chemistry Department UMT, for her learned guidance and kind behavior during the course of my study.

I am most thankful to my supervisor and my inspiration Dr. Mohsin Javed not only for providing me opportunity to do my research work but also for his dynamic elaborate instructions, enlightening suggestions, illustrious advices, and persistent help and clarifying my concepts relating to course work and guiding me at each and every step of this research work.

In last, especially I want to thank my research fellow Naveed Ahmad & Asma Iqbal for their extraordinary support in completion of this research work.

May Allah bless all of these people!

(Ishrat Fatima)

ABSTRACT

Pure zinc oxide and Cr-doped ZnO nanoparticles were prepared via hydrothermal route. In Cr-doped ZnO nanoparticles a series of doped nanoparticles (1, 3, 5, 7 and 9% by mol) was prepared. These prepared nanoparticles were characterize by FTIR, SEM and XRD to check the morphology of synthesized nanoparticles then further used in photocatalytic activity for Methylene Blue standard dye degradation. Results of photocatalytic activity showed that 5% Cr-doped ZnO nanoparticles exhibited excellent dye degradation in sunlight. Graphitic carbon nitride was synthesized from thermal degradation of thiourea. Graphitic carbon nitride used for photocatalytic activity also showed good results for methylene blue standard dye degradation. To enhance the photocatalytic activity of Cr-doped ZnO nanocomposite series (5, 10, 15 and 20%) was synthesized from 5% Cr-doped ZnO nanoparticles and g-C3N4. The prepared nanocomposites were characterized to confirm the synthesis and morphology of prepared nanocomposites and used in photocatalysis. UV-Vis spectroscopy, Tauc plots, FTIR, XRD and SEM were used to characterize nanoparticles and nanocomposites. Attained results explain that best dye degradation was observed in 15% nanocomposite which possesses 2.4 eV band gap lower than ZnO and g-C3N4.