We dedicate our project to the employees and workers who are suffering from low facilities and wages, but putting high efforts for the survival of textile industry.

# Acknowledgement

# Firstly, we are very thankful to Allah Almighty for giving us a precious chance to work on this project.

# Secondly, it is a pleasure to thank those who made this project possible, the honorable Our Project supervisor Dr. Nabeel Amin and External-Supervisor Mr. Tanveer Alvi for helping us in the selection of a useful topic for textile industry and giving us their opinions and help us in this project.

# Mohammad Abad

# Osama Tayyab

Abstract

The main purpose of this project is the studying of seam stitches and finishing faults in the garments and then prepares the samples of seam stitches and finishing faulted garments and products and then checks the faults of samples by doing standard testing methods. Regarding to this project the study of all possible remedies through the standard testing methods applied for the different type of seams stitches, their problems and their solutions and also to conclude and get the best remedies which can be apply  after getting standard testing results.

Table of content

Topic										   Page No.

# Chapter 1

# 1.1- Introduction…………………………………………………………………………………02

1.2- Objectives…………………………………………………………………………………..02

1.3- Literature review…………………………………………………………………………….02

# 1.4 Apparel/Clothing…………………………………………………………………………….03

1.5- Sewing……………………………………………………………………………………....03

# 1.6- Sewing Machines…………………………………………………………………………...04

# 1.7- Types of Sewing Machines………………………………………………………………….04

### 1.7.1- Mechanical Sewing Machines…………………………………………………….05

### 1.7.2- Electronic Sewing Machines……………………………………………………..05

### 1.7.3- Computerized Sewing Machines………………………………………………….05

1.8- Main Stitching Machines……………………………………………………………………05

1.8.1- Chain stitch Machines…………………………………………………………….05

1.8.2- Lock stitch Machines……………………………………………………………..06

# 1.8.3- Overlock Machines……………………………………………………………….07

## 1.9- Stitch formation……………………………………………………………………………..09

# 1.10- Seam……………………………………………………………………………………….10

# 1.11.1- Types of Seam…………………………………………………………………………...10

1.11.1- Decorative Seam…………………………………………………………………10

1.11.2- Super Imposed Seam…………………………………………………………….10

1.11.3- Applied Seam……………………………………………………………………10

1.11.4- Bound Seam ……………………………………………………………………..10

1.11.5- Single Ply Construction Seam…………………………………………………...10

# 1.11.6- Edge Neatening…………………………………………………………………..10

1.11.7- Lapped Seam…………………………………………………………………….11

# 1.12- Factors associated with Seam and stitches………………………………………………...11

1.12.1- Sewing needle……………………………………………………………………11

1.12.2- Fabric type and weight...………………………………………………………...11

1.12.3- Type of thread…………………………………………………………………...11

1.12.4- Thread construction……………………………………………………………...12

# 1.12.5- Thread tension or Stitch balance………………………………………………...12

# 1.13- Seam Class Guide………………………………………………………………………….12

# 1.13.1- Superimposed Seams…………………………………………………………….13

# 1.13.2-Lapped Seams…………………………………………………………………….14

# 1.13.3-Bound Seams……………………………………………………………………..15

# 1.13.4-Flat Seams………………………………………………………………………...16

# 1.13.5-Edge Finish Stitching……………………………………………………………..18

# 1.13.6Ornamental Stitching……………………………………………………………...19

# 1.14-Stitching…………………………………………………………………………………….20

# 1.14.1- Stitch Class Guide……………………………………………………………….20

# 1.14.2-	100 Class Stitches………………………………………………………………..21

# 1.14.3-	200 Class Stitches………………………………………………………………..21

# 1.14.4-	300 Class Stitches………………………………………………………………..22

# 1.14.5-	400 Class Stitches………………………………………………………………..23

# 1.14.6-	500 Class Stitches………………………………………………………………..23

# 1.14.7-	600 Class Stitches………………………………………………………………..24

# 1.14.8-	Button Hole Stitches……………………………………………………………..25

# 1.15- Seam Stitches faults and their causes……………………………………………………...26

1.15.1- Staggered stitch…………………………………………………………………..26

# 1.15.2- Insecure back stitching…………………………………………………………..27

1.15.3- Twisted seams leading to irregular puckering…………………………………...27

# 1.15.4- Poor seam locking……………………………………………………………….28

1.15.5- Seam failure due to fabric breakage……………………………………………..28

# 1.15.6- Loose stitches……………………………………………………………………29

# 1.15.7- Improperly formed stitches………………………………………………………29

# 1.15.8- Crowded stitches…………………………………………………………………30

# 1.16- Some common seam and stitching problems……………………………………………...30

# 1.16.1- Seam Puckering………………………………………………………………….31

1.16.1.1- Yarn Displacement or Structural Damage……………………………..31

# 1.16.1.2- Thread Tension Puckering……………………………………………..32

1.16.1.3- Feed Puckering (Uneven Ply Feeding) ………………………………..33

# 1.16.1.4- Shrinkage Puckering…………………………………………………...35

# 1.16.2- Seam Grin…………………………..……………………………………………35

# 1.16.3- Seam Slippage…………………………………………………………….……..36

# 1.16.4- Skip stitch………………………………………………………………………..36

# 1.16.5- Unbalanced stitches……………………………………………………………...37

# 1.16.6- Variable Stitch Density…………………………………………………………..37

# 1.16.7- Fabric Flagging…………………………………………………………………..38

# 1.17- Finishing…………………………………………………………………………………...38

# 1.17.1- Seam Finishes……………………………………………………………………38

# 1.17.2- Types of finishes…………………………………………………………………38

1.17.2.1- Pinked Seam Finish……………………………………………………………38

1.17.2.2- Stitched and Pinked Seam Finish……………………………………………...39

1.17.2.3- Zigzagged Seam Finish………………………………………………………..39

1.17.2.4- Overcast/Over edged Seam Finish…………………………………………….39

1.17.2.5- Clean-finished Seam…………………………………………………………...40

1.17.2.6- Bound Seam Finish…………………………………………………………….40

1.17.2.7- Flat-felled Seam Finish………………………………………………………...40

1.17.2.8- Hong Kong Seam Finish……………………………………………………….40

1.17.2.9- Finishing Inside Seams………………………………………………………...41

1.17.2.10- French seam…………………………………………………………………..41

1.17.2.11- Flat-fell seam…………………………………………………………………41

# 1.17.3- Seam Finishes uses………………………………………………………………………42

# Chapter No 2

# Testing and experimental work…………………………..………………………………………44

# 2.1Testing………………………………………………………………………………………...44

# 2.2 Seam stitching tests…………………………………………………………………………..44

# 2.2.1 Seam strength test………………………………………………………………….44

2.2.2 Seam Slippage Test………………………………………………………………...47

# Chapter No 3

3. Research Methodology……………………………………………………….……………….53

Reference ……………………………………………………………………………………….54