“Vat Dye printing on Cellulosic fabric with reactive dye”

Project Advisor

Mr. HASEEB AKRAM

Presented By

Muhammad Ramzan

ID # 091420131

Muhammad Usman Akhtar

ID # 091420192

Abdul Qadeer

ID# 071020105

Session 2009 – 2013

School of Textile and Design

University of Management and Technology

DEDICATION

First of all I dedicate my project to the greatest personality in the universe Hazrat Muhammad (S.A.W). Secondly, I dedicate my project to mygreatest blessing: my parents, for every effort they made to make us happy, for every prayer they offered for me, for every second of their lives they dedicated to me!!! What I am today is because of them!!!

Teachers especially to my kind supervisor Mr. Haseeb Akram, Due to their desire, care, affection and our keen interest, I achieved this level of excellence where I am looking for most bright future ahead.

May Allah bless all of them with everything He has ever created and may give me an opportunity to serve them the best way possible……. (Ameen)

ACKNOWLEDGEMENT

All the praises are for the almighty, Allah who bestowed me with the ability and potential to complete this project.

Words are very few to express enormous humble obligations to my affectionate Parents for their prayers and strong determination to enabling me to achieve this job.

I take this opportunity to record my deep sense of gratitude and appreciation to my project Advisor Mr. Haseeb Akram, School of Textile&Design, U.M.T Lahore for his constant encouragement and inspiring guidance with her Wisdom. at all times to enable us to work on this project His support, encouragement, and guidance have been invaluable in the successful completion of this project report. He has been most patient and helpful all through in all our endeavors to learn more during our project work. I also want to thank

Dr. NABEEL AMEEN Director School of Textile and Design.

We are also thankful to our families for being beside us and encouraging us in all that wehave been doing. We thank UMT for educating us in various ways, and for providing me with the good education there is. We would like to take the opportunity to thank the faculty and staff for helping us prepare for a life after graduation. Not everyone is so fortunate. We know we still have much to learn, but with continued support and encouragement from people like you we know we can accomplish a great deal. We have learnt new things all along the process and we thank everyone for their support and advice.

ABSTRACT

Discharge Printing is one of the recently generated printing. This print is a style of printing.Structure of discharge print is different from others printing styles. The main difference which distinguish it from others styles is the use of reducing agents. Sodium hydro sulfite was used as a reducing agent. The discharge print fabric has good textured. The faults arising in this printing style is due to the conditions which are not suitable for this. Discharge fabrics were preprocessed by different dyeing methods (i.e. exhaust and continuous) to apply discharge effects. Two different types of this style is discussed white discharge, and color discharge. There were no Cross-linking agents (binders used in pigment printing) applied before and after printing. The discharge paste is printed on to the dyed fabric and, usually during subsequent steaming; the dye in the pattern area is discharged. A white discharge is thus produced.

Discharge is usually a water-based screen printing method. The majority of the ink has a water based component as its base. Water-based discharge prints can achieve the opacity of plastisol in addition to a very soft hand on dark-colored garments. It enables light, brighter colors to be obtained on a dark ground and Very sharp features like fine outlines, dots, raster etc., can be produced with total clarity, without any smudging (due to overlapping of contact colors) or outfitting problems normally faced by direct style of printing. The effect, clarity, distinction, richness and aesthetic appeal obtained add value for discharge printing. It is an expensive process with two stage application involved in dyeing or padding and discharge printing and most important results was Limited choice of ground and motif colors. Only dischargeable dyes can be discharged by this method. But in the color discharge printing we use different type of the color. When we use the vat dye color in the discharge printing that is little bit different form the white discharge in the vat discharge print cycle is print, dry, chemical pad, flash ageing, 
and Re- oxidation then washing.